Military B-Series Breakout Mil-Tac Cable 24G62,5/125μ

\*\*tde - Mil-Tac Cable

Applications: Mil-Tac cables are ideal for use in harsh environments where deployment and retrieval for reuse is required.
• Extremely strong, lightweight, rugged, survivable tight-buffered cables designed for military tactical field use and commercial applications
• Compact, round cable design for ease of transportation and deployment
• Designed for use in adverse environments where reduced size and weight are important
• Helically stranded cable core for flexibility, deployment survivability and exceptional mechanical protection for the optical fibers
• Cables have been tested and are in use in military data communications applications worldwide
• Can be used outdoors for temporary deployment directly on the ground in all terrains, including severe environments
• Suitable for industrial, mining and petrochemical environments
• Crush-resistant and resilient with a thick layer of aramid strength members
• Polyurethane jacketed for abrasion, cut and chemical resistance

\*\*FO Cables

\*\*TECHNISCHE\_DATEN

|  |  |
| --- | --- |
| Impact Resistance | 200 Impacts |
| Crush Resistance | 440 N/cm |
| Flex Resistance | 2.000 Cycles |
| Operating Temperature | -55°C to +85°C |
| Storage Temperature | -70°C to +85°C |

|  |  |
| --- | --- |
| Fiber Count | 24 |
| Diameter | 14.5 mm (0.57 in) |
| Weight | 150 kg/km (101 lbs/1.000`) |
| Installation Tensile Load | 9.600 N (2.160 lbs) |
| Operational Tensile Load | 2.400 N (540 lbs) |
| Minimum Bend Radius Installation | 23.2 cm (9.1 in) |
| Minimum Bend Radius Operational | 11.6 cm (4.6 in) |