Military B-Series Breakout Mil-Tac Cable 2E9/125μ G.652.A

\*\*tde - Mil-Tac Cable

Applications: Mil-Tac cables are ideal for use in harsh environments where deployment and retrieval for reuse is required.
• Extremely strong, lightweight, rugged, survivable tight-buffered cables designed for military tactical field use and commercial applications
• Compact, round cable design for ease of transportation and deployment
• Designed for use in adverse environments where reduced size and weight are important
• Helically stranded cable core for flexibility, deployment survivability and exceptional mechanical protection for the optical fibers
• Cables have been tested and are in use in military data communications applications worldwide
• Can be used outdoors for temporary deployment directly on the ground in all terrains, including severe environments
• Suitable for industrial, mining and petrochemical environments
• Crush-resistant and resilient with a thick layer of aramid strength members
• Polyurethane jacketed for abrasion, cut and chemical resistance

\*\*FO Cables

\*\*TECHNISCHE\_DATEN

|  |  |
| --- | --- |
| Impact Resistance | 1.500 Impacts |
| Crush Resistance | 2.200 N/cm |
| Flex Resistance | 2.000 Cycles |
| Operating Temperature | -55°C to +85°C |
| Storage Temperature | -70°C to +85°C |

|  |  |
| --- | --- |
| Fiber Count | 2 |
| Diameter | 6.5 mm |
| Weight | 36 kg/km |
| Installation Tensile Load | 2.200 N |
| Operational Tensile Load | 550 N |
| Minimum Bend Radius Installation | 6.5 cm |
| Minimum Bend Radius Operational | 3.3 cm |